## Slide 1
Best Practices in Usage of RMC in Infra Projects
28th November 2018
Additional focus - Developments in Performance oriented Concrete
devendra.pandey@adityabirla.com
Notes: Font for the entire presentation to be changed. The font must look big and bright. The aspect ratio of all our brand logos to be kept as per the original format.

## Slide 2: Ready Mixed Advantage for BETTER Concrete Four legged approach
Produce better
Handle better
Protect better
Specify better

## Slide 3
UltraTech RMC Plants
Chandigarh
Gurgaon
Noida
Jaipur
Lucknow
Kolkata
Vizag
Raipur
Nagpur
Vijaywada
Hyderabad
Tirupati
Chennai
Coimbatore
Cochin
Mysore
Mangalore
Bangalore
Goa
Kolhapur
Mumbai
Pune
Nasik
Indore
Bhopal
Ahmedabad
Rajkot
Notes: Colour of the map to be of a darker shade. Back ground to be of our RMC plant to be used. Location icons to be of a brighter colour

## Slide 4
IT Systems
Production Management (SAP)
Quality Management (Labsys)
Outbound Logistics (Vehicle Tracking System/M Zone)
Integration with Finance Management (SAP)
Quality Assurance and Control
Standardized processes to ensure quality production
Strong Quality Management Systems
Superior quality Control leveraging IT Systems
UltraTech Concrete With World Class Manufacturing
World Class Manufacturing
A Blend of Superior IT Systems, Manpower, Quality assurance and control and customer focus has led us to this position of World Class Manufacturer
Notes: UltraTech RMC plant image to be inserted

## Slide 5
UltraTech Concrete Advantage
Assured Quality Always
Centralized Mix Approval
Raw Material Characteristic database and Analysis
Mix Design: Flexibility in Design Methodology
QCI Certified RMC plants
Centralized Database: Concrete Strength
Notes: No change. Use RMC logo

## Slide 6: QC processes for consistent quality
Sourcing of the best quality raw material
Well documented and consistent raw material testing processes.
Centralized control of mix recipes integrated to the Batching system
Tests in the plant prior to dispatch of concrete to customers sites.
Testing of concrete at site prior to pumping / application.
Pour card to maintain traceability of concrete poured at site.

## Slide 9: Hardened concrete testing processes
Proper sampling & mixing
Interfaced migration of data into LABSYS

## Slide 10: Ready Mixed Advantage for BETTER Concrete Four legged approach
Produce better
Handle better
Protect better
Specify better

## Slide 11: Placing Concrete – Many methods!

## Slide 12: Concrete Pumping
Pump Placement
Ttransit mixer movement planning
Pump levelling
Minimum bends
Sturdy shuttering
Vertical clamping
Support manpower & equipment
Pour from extreme end

## Slide 14: Workability works !!!

## Slide 15: Re-tempering of RMC

## Slide 16
(Water+admixture)

## Slide 17: COMPACTION OF CONCRETE
  Consequences of entrapped air
    5% voids reduces ---- 30% strength of concrete
    10% voids reduce ---- 50% strength of concrete

## Slide 20: Sampling !!! This is a very important issue !!!
“ Sampling and testing of concrete is an engineering art.”
Poor sampling and handling -- inconsistent and false results
Truly random basis
Instead of sampling concrete microscopically - ensure representative-ness
Remix thoroughly
AVERAGE
REMIX
SAMPLE THROUGH THE LOAD
2 TESTS
AT LEAST 3 INCREAMENTS

## Slide 21: Point to Reflect : Slump or Workability??

## Slide 22: Definition of ‘Sample’ (Clause 6.3.2 of IS 4926-2003)
Is one cube a ‘sample’? …… NO!
Should we find an average of strengths from cubes of different samples? …… NO!
Should we take samples from every TM? …… NO! (1 every 50 Cum)
For reduced errors, cast more cubes from lesser samples

## Slide 23: Testing compressive strength
Calibration
Bottom platen – horizontal, plane
Top platen – swivel
Do not place on casting faces
True failures
One sided or Abnormal failures

## Slide 24: Cube Strength Failures POOR CONCRETE ? OR POOR TESTING ?

## Slide 25
-40
-30
-20
-10
0
+10
%
TRUE AVERAGE CUBE STRENGTH OF
BATCH OF CONCRETE (BS 1881)
SAMPLING ERROR
FAILURE TO REMIX SAMPLE
DISTORTED CUBE MOULD; LACK OF
MOULD OIL
INCOMPLETE COMPACTION OF CONCRETE
CURING TEMPERATURE OUTSIDE
OF PERMITTED RANGE
LACK OF CONTINUOUS
MOIST CURING
FAULTY CUBE LOCATION IN MACHINE OR
OTHER OPERATOR FAULT
FAULTY TEST MACHINE
Strength of cube relative to true
average cube strength of batch of concrete

## Slide 26: Diagnostics – CBC count!
Unsymmetrical Failure Pattern
Variation in individual cube weights, strengths
Horizontal cracks / Cracks on top or bottom surface
Extreme variation in test results of cubes from the same sample
Poor repeatability / Vague results
% Variation

## Slide 27: CORRECTIVE ACTIONS
Low average strength & High Standard Deviations
  Rework the design, Reevaluate the supplier
Medium average strengths (> Fck+3) & Low standard deviation
  No change, optimized concrete
Low average strengths (< Fck+3) & Low standard deviation
  Increase Cement content, reduce w/c
Low strengths coupled with unpredictable results & symptoms of testing errors
  Check testing equipment condition & calibration, Use trained manpower for sampling & testing
  No change in design, Verify tests done by RMC supplier
Low average strength & High within sample variation
  Discard lower results, find the average of remaining cubes
Two sets of extremely varying results – one passing, one failing
  Accept the high result & investigate the reason for discrepancy

## Slide 28: Quality Control - Macro
Statistical control and the variability – Standard Deviation
Recognition of testing errors, leading to discarding of low result
Attempt to ensure that no unsatisfactory concrete is produced rather than to try to detect individual unsatisfactory truckloads.
Recognition that the concrete supplier is in a far better position to control his concrete than the purchaser, leading to certification of suppliers instead of control of supplied concrete by purchaser - QCI

## Slide 29: Ready Mixed Advantage for BETTER Concrete Four legged approach
Produce better
Handle better
Protect better
Specify better

## Slide 33: Theory of Plastic Shrinkage Cracking
TIME
S
T
R
A
I
N
SETTING
PERIOD
CONCRETE WITH FIBRES
RMC without
early protection
TENSILE STRAIN CAPACITY
PLASTIC SHRINKAGE STRAIN
REGULAR RMC
Well cured RMC

## Slide 34: Please Protect the Baby

## Slide 35: Prevention is the Real Cure

## Slide 36: Ready Mixed Advantage for BETTER Concrete Four legged approach
Produce better
Handle better
Protect better
Specify better

## Slide 37: Are all plants same as RMC?

## Slide 38: Some queries to resolve!
What about NDT or core tests?
  More chances of error than cubes !
Can we prescribe our own mix design?
  Uneconomical & no performance guarantee
Does fly ash / GGBS addition mean inferior or cheaper concrete?
  Do we spend more to have a longer life? DURABILITY !

## Slide 39
Made to Order
Raw Material Characteristic database and Analysis
Centralized Mix Design Approval
Mix Design
Tracking
Mix Design: Flexibility in Design Methodology
Online Design mix development and analysis
Batching
Scheduling
UltraTech Concrete
Key Processes

## Slide 40
Site Based Activities
Training programmes on cement & concrete technology for site Managers & Engineers
Assistance on regular field construction related queries.
Field Demo & Guidance on Good Construction Practices.
Training of Quality Control Team / Lab Technicians on cement testing by our experienced plant Q/C personnel
Training of QC team / Lab team on concrete testing
Notes: Attractive font to be used

## Slide 41
UltraTech Specialty Concrete Offerings
Notes: Logos to be as per our brand guidelines. Logo to be used from artwork files

## Slide 42
UltraTech Specialty Concrete Offerings
Notes: Logos to be as per our brand guidelines. Logo to be used from artwork files

## Slide 43
A Self Compacting Concrete designed to flow freely irrespective of the dense reinforcement and complexity of the structure
M60 Freeflow in deck slab of Cable Stayed Bridge for Mumbai Metro over Western Express Highway
Notes: Slides to be formatted

## Slide 44
Mumbai Metro
Average Strength-80 MPa
Standard Deviation- 4 MPa
A special high performance concrete designed for slender structure which bear heavy loads
Notes: Slides to be formatted

## Slide 45
Mumbai Mono Rail
  Avg. RCPT Value- 900Coulombs @ 28 days
  Permeability- 10 mm @ 28 days
A specially designed High Performance Concrete for extra durable structures
Chennai Metro
  Avg. RCPT Value- 750 Coulombs @ 28 days
  Permeability- 8-9 mm @ 28 days
Notes: Slides to be formatted. Mumbai Mono rail to be 1st

## Slide 46: Crystalline waterproofing for freedom from dampness

## Slide 47
Lite is light weight concrete which is 50-75% lighter than normal concrete. It has
thermal insulating properties & sound insulation. It has improved thermal properties,
reduced structural loading and fire resistant.
Standard Concrete Specification:-
Strength class | 1-25 MPa
Viscosity | Low
Slump | 120 – 200mm
Segregation resistance | High
Density | 650 kg/m3 & above
Light Weight Concrete for Insulating walls and fills

## Slide 48
Stamped Concrete for Landscaping
Decor is a range of concrete to be printed or stamped for making decorative surfaces on porch, paving. It can be designed from M25 to M35 MPa compressive strength at 28 days as per the requirement. Higher grades are also available if required. The aesthetic results are achieved by affixing moulds or stencils on fresh concrete surface phase curing. The final appearance resembles that of natural materials such as stone and wood.
Standard Concrete Specification:-
Strength class | 25 – 35 MPa
Workability | Can be designed as per the requirement

## Slide 49: Bucket Concrete for small usages, repair work
Bucket concrete is the normal concrete (M15 to M35 grade) delivered in 15/10 litres bucket at the site or picked up at any of our plants. It can be transported on any vehicle.
Strength class | 5 – 40 MPa
Workability | Can be designed as per the requirement

## Slide 50
Glimpse Of Our Valued Customers

## Slide 51
Thank You !